## Slide 1: EE207 P-N Junction Diode
S. Lodha
From: R. Pierret, Semiconductor Device Fundamentals

## Slide 2: P-n Junction Equilibrium Band Diagram
At equilibrium

## Slide 3: P-n Junction Electrostatic Picture
At equilibrium
Built-in potential, electric field and charge density

## Slide 4: Built-in potential

## Slide 5: Depletion Approximation
Simpler solution to Poisson’s equation

## Slide 6: Quantitative electrostatics

## Slide 7: xn, xp
Continuity of E and V at x=0
  No sheet charge or dipole at x=0

## Slide 8: Applied voltage VA
Under low level injection and low R Ohmic contacts, VA drops across the depletion region

## Slide 9: Electrostatics
Replace Vbi with Vbi-VA

## Slide 10: Electrostatics
Depletion width, electric field and potential drop increase if VA<0 and decrease if VA>0

## Slide 11: Band diagrams
Forward bias (VA>0
Reverse bias (VA>0)
Quasi-fermi levels not drawn in depletion region

## Slide 12: Current flow (Band diagrams)

## Slide 13: Full Circuit Picture
Net current is constant, Jn(x) and Jp(x) vary with x
Steady state, dn/dt = dp/dt =0

## Slide 14: Current and carrier densities
Forward Bias
Reverse Bias

## Slide 17: Experimental I-V
Break down at high RB
Higher than expected currents at low FB and RB
Non-saturating RB current
Slope decreases at high FB

## Slide 18: Avalanche Breakdown
Lower doping gives higher VBR
Larger bandgap gives higher VBR
Higher T requires higher VBR

## Slide 19: Zener Breakdown
Higher reverse bias V increases number of electrons and available states
Higher doping decreases tunneling width

## Slide 20: R-G current
Note dependence on W (RB) and ni

## Slide 21: Series Resistance

## Slide 22: High Level Injection
Typically not seen, since Rs effect kicks in much before HLI sets in

## Slide 23: Reverse-bias admittance
G is approx zero
Variable capacitance in reverse bias due to majority carriers

## Slide 24: Transient off response
Current flips to large –ve current
Storage time is most important
  Depends on IF, IR, τp

## Slide 25: Transient-off
Excess Minority charge is removed through recombination (limited by τp) or current flowing out (limited by IR)

## Slide 26: Optoelectronic diodes
Wavelength (um)=1.24/EG(eV)

## Slide 27: PN jn photodiode
Generation of reverse current

## Slide 28: P-i-n photodiode
Fmax high (~GHz) since carriers are quickly swept away by e-field
Response tuned by width of i-layer

## Slide 29: Solar cells
Energy loss and cost are the main drivers of solar technology (price / watt)

## Slide 30: LEDs
Band-band recombination in forward bias
Three requirements:
  Direct Band gap
  1.77 eV< EG < 3.1 eV
  Ability to form pn junctions

## Slide 31: Commercial LEDs