## Slide 1: EE 207: BJTs
S. Lodha
From: R. Pierret, Semiconductor Device Fundamentals

## Slide 2: NPN and PNP BJTs
Only two independent voltages and currents

## Slide 3: Device Cross-section
Double-diffused discrete pnp BJT

## Slide 4: Device Cross-section
BJT in an integrated circuit
  Device isolation is critical
  All contacts at the top

## Slide 5: Biasing Modes
Amplifier in active mode
Switch in cut-off and saturation regimes

## Slide 6: Operation of BJT
Active mode biasing

## Slide 7: Amplification
Common emitter mode
Small base electron current controls the large hole collector current

## Slide 8: Ideal BJT solution
Similar to the ideal diode case, solve MCDE in three quasi-neutral regions

## Slide 9: Strategy
Solve MCDE in each QN region with appropriate boundary conditions
Emitter:
Base:
Collector:

## Slide 10: Strategy (contd.)

## Slide 11: Solution
The solution in the base region is similar to narrow-width diode
Emitter:
Base:
Collector:

## Slide 12: Solution (contd.)

## Slide 13: W<<LB
No recombination  Linear dependence

## Slide 14: BJT parameters
Higher emitter doping improves ϒ
Smaller W improves βdc

## Slide 15: Ebers-Moll DC circuit
DC equivalent circuit

## Slide 16: Ebers-Moll DC circuit
Used in circuit simulation software
Show that αF= αDC

## Slide 17: Theory vs Experiment
VCB dependence of IE
IC increase for large VCB

## Slide 18: Theory vs experiment
Increase in IC with VEC
Breakdown at VCE0 < VCB0

## Slide 19: Base-width modulation
Quasi-neutral base width is a function of applied biases
Also known as “Early effect” after J. Early

## Slide 20: Punchthrough
Extreme case of BWM, W 0
Small increase in –VCB leads to exponential increase in carriers injected over the ‘hill”

## Slide 21: Avalanche breakdown
Common emitter breakdown voltage (VEB0) < Common base breakdown voltage (VCB0)

## Slide 22: Series Resistances
rB is the most significant since it causes VEB to decrease
  VEB’=VEB-IBrB

## Slide 23: Emitter current crowding
Injection current highest at the emitter edges
  Can cause local heating at high current levels

## Slide 24: Graded Base
Graded doping in base leads to an electric field
  Aids minority carrier transport in the base

## Slide 25: Gummel plot
Ratio of IC/IB gives βdc

## Slide 26: Poly emitter BJT
Lower mobility in poly-emitter reduces electron injection current and increases ϒ

## Slide 27: Heterojunction Bipolar Transistors
Typical heterojunction emitter-base combinations
Abrupt
Graded

## Slide 28: HBT Advantage
Wide emitter allows NE << NB
Higher base doping lowers rB, current crowding and base-width modulation

## Slide 29: Examples

## Slide 30: Problem 1

## Slide 31: Problem 2

## Slide 32: Solution Problem 2
Two back-to-back diodes

## Slide 33: Problem 3

## Slide 34: Solution 3

## Slide 35: Problem 4
For a narrow base p+ n p BJT:
  Using the carrier profile picture show the impact of W reduction on Υ, αT, αdc, βdc
  Show the impact of reduction in LE on Υ, αT, αdc, βdc

## Slide 36: Problem 5
Assuming a narrow base P+/n/P- BJT, draw the minority carrier distribution in the E, B, and C regions if VCE=0 and IB>0. Comment on relative magnitudes of IC and IE.
  Using the Ebers Moll model, express IC in terms of EB parameters and the E-B voltage, VCE=0
  Noting the relative magnitudes of the EB parameters (assuming a P+ n p- structure) discuss how IC depends on IB at VCE=0. Do the curves pass through the origin?