## Slide 1: EE207 Solid State Devices
S. Lodha
Carrier Statistics
Supplementary Slides
Acknowledgements:
Advanced Semiconductor Fundamentals, R. Pierret, Purdue University

## Slide 2: Carrier Distributions

## Slide 3: Energy Band Diagrams
Quote from Herbert Kroemer (Nobel Prize in Physics, 2000)

## Slide 4: Impurities
Energy levels for various impurities

## Slide 5: Fermi Dirac Integral

## Slide 6: Intrinsic Carrier Conc

## Slide 7: Concentration vs T

## Slide 8: Fermi level position vs doping

## Slide 9: Problem 1

## Slide 10: Problem 2

## Slide 11: Problem 3
At T=300 K, a p-type semiconductor (NA≠0, ND=0) is doped in such a way that it is at the threshold of becoming degenerate. Find out the position of the Fermi level of this semiconductor at T=450 C. Assume at T=300 K, ni = 108 cm-3, EG=1.25 eV, kT =25 meV and equal effective masses for electrons and holes. Also assume that the band gap is independent of temperature