## Slide 1: EE 207: MOS Fundamentals
S. Lodha
From: R. Pierret, Semiconductor Device Fundamentals

## Slide 2: MOS Capacitor
Ideal capacitor

## Slide 3: N-type MIS
Block charge diagrams

## Slide 4: Definitions of potentials
ɸF>0 for p-type semiconductor
ɸF<0 for n-type semiconductor

## Slide 5: Variation in ɸs>0 for p-type semiconductor
The variation for n-type will be the negative of the variation for p-type

## Slide 6: Actual Solution
Accumulation and Depletion in p-type Si

## Slide 7: Actual solution
At and beyond inversion in p-type Si

## Slide 8: Vg vs φs
Delta depletion vs exact
Little modulation of φs in accumulation / inversion with increase in Vg
  All voltage drop across oxide

## Slide 9: MOS C-V Charge Analysis

## Slide 10: Effect of doping variation
Increased Cmin and wider depletion region in the C-V
Flat for heavily doped (semiconductor is like metal plate)

## Slide 11: Effect of oxide thickness
Increasing Cmin, wider depletion region of C-V
  Increase in voltage drop across the oxide with thicker oxides

## Slide 12: Effect of temperature

## Slide 13: Deep depletion
Faster ramp rates do not allow enough time for minority charge to appear
  Depletion region widens to uncover positive charge

## Slide 14: Non ideality: φms≠0
Flat band voltage shift

## Slide 15: Non-ideality: Fixed charge
Oxidation condition dependent
Post N2 anneal helps
Adds to flat-band voltage shift

## Slide 16: Non-ideality: Mobile ions
Alkali ions that move with applied bias and temperature

## Slide 17: Non-ideality: Mobile ions
Gettering or charge neutralization

## Slide 18: Non-ideality: Interface states
C-V stretch out
Acceptor-like traps in upper half of band-gap
Donor-like traps in lower half of band-gap

## Slide 19: Interface traps
H2 anneal passivates dangling bonds
Midgap Dit ~ 1010 states/cm2 eV

## Slide 20: State of the art gate stack
Silicon substrate
Gate
3.0nm High-k
Silicon substrate
1.2nm SiO2
Gate